Title: From waste to value: agricultural input production from zinc industry residues

Topic: Waste management and circular economy

Category: 4. ESG (Environmental, Social, Governance)

Authors:

- Isabela Correia Costa; Nexa Resources; Innovation Analyst; Sergipe Street, 1440, 8° floor - Savassi, Belo Horizonte, Minas Gerais, Brazil; Zip code 30130-174; ext.isabela.costa.ic1@nexaresources.com; +55 31 99832-0500.

- Saulo Luiz Sales Parreiras de Rezende, Nexa Resources, Innovation Engineer, ext.saulo.rezende@nexaresources.com, +55 31 99876-2819.

- Henrique Hipólito Costa, Nexa Resources, Innovation Engineer, ext.henrique.costa@nexaresources.com, +55 31 99141-5230.

Key words: zinc residue; agricultural inputs; circular economy; sustainable production; mining waste valorization; zinc-based fertilizer.

Abstract:

According to the Brazilian Mining Institute (IBRAM), in 2024, the mineral trade balance represented 47% of Brazil’s total trade balance, highlighting the sector's economic relevance (IBRAM, 2024). However, the mineral production chain generates significant waste, as explained in the 2017 Inventory of Solid Mining Waste, published by the Minas Gerais State Environmental Foundation (FEAM), which indicated the generation of more than 562 million tons of mining waste in the state (FEAM, 2018).

Alongside this, the agribusiness sector accounts for 24% of Brazil's wealth generation and has a strong influence on the country's GDP (EMBRAPA, 2023). Currently, there is an urgent need to reconcile accelerated population growth, which increases the demand for food, with the preservation of ecosystems, encouraging investments in sustainable intensification techniques (EMBRAPA, 2018). One such practice is soil acidity correction, which enhances nutrient availability and reduces toxic element solubility.

Considering the above, this work aims to develop a new agricultural input from the processing of a dolomitic residue generated in the beneficiation of zinc ore and another residue generated in the wastewater treatment of a zinc smelter. The agricultural input to be produced consists of a combination of limestone and gypsum, simultaneously guaranteeing the correction of soil acidity, the supply of essential micronutrients (calcium, magnesium and sulphur) and the neutralization of toxic aluminum in deeper layers (VITERAGRO, 2022). The product generated also has the potential to provide zinc, an essential micronutrient for plant growth and development.

To be commercialized, the material must meet the specifications of the Ministry of Agriculture and Livestock (MAPA), with regards to the maximum concentrations allowed for toxic heavy metals and other substances. Annex I of MAPA Normative Instruction No. 27 stipulates that, for mineral fertilizers containing secondary macronutrients and micronutrients, the maximum permissible levels of cadmium and lead must be calculated by multiplying the sum of the guaranteed micronutrient percentages in the fertilizer by 15 and 750, respectively. The resulting values correspond to the contaminant content in mg/kg of fertilizer (BRASIL, 2006). As Table 1 shows, the waste described above has cadmium and lead levels above those permitted by current legislation, according to analyses carried out by atomic absorption. Therefore, it is necessary to subject the material to a treatment process to ensure its compliance with market requirements. The process involves treatment in a rotary kiln to remove the contaminants.

Table 1. Characterization of the residue under study.

| Residue | Residue 1 - zinc ore beneficiation | Residue 2 – wastewater treatment from zinc smelter |
| --- | --- | --- |
| Zn content (%m/m) | 3,2 | 21,9 |
| Cd content (ppm) | 400 | 3000 |
| Cd Limit (ppm) | 45 | 300 |
| Pb content (ppm) | 3000 | 5400 |
| Pb Limit (ppm) | 2250 | 10000 |

The methodology for evaluating the proposed technology involved conducting tests in a pilot-scale rotary kiln with a feed capacity of 10 kg/h, a length of 4 m, a rotation speed of 0.0056 Hz, and an inclination of 2°. Two tests were performed in duplicate, as detailed in Table 2. The kiln was fed with a mixture of the two residues, along with calcium chloride—used to facilitate lead removal—and coke. The coke mass flow rate varied from 27% to 10%, a condition aimed at ensuring the economic feasibility of the process. Each experiment had a residence time of 24 hours, and the average kiln temperature was maintained at 990°C, which exceeds the decomposition temperature of the dolomite matrix (approximately 900°C) (Olszak-Humienik, 2015). The material obtained after each test was collected and subjected to atomic absorption spectroscopy for contaminant analysis.

Table 2. Conditions of the tests conducted in a pilot-scale rotary kiln.

| Condition | Residue 1 (kg/h) | Residue 2 (kg/h) | CaCl2 (kg/h) | Coke (kg/h) |
| --- | --- | --- | --- | --- |
| 1 | 2,8 | 4,3 | 0,2 | 2,7 |
| 2 | 4,5 | 4,3 | 0,2 | 1,0 |

Based on the average of the duplicates, the results indicated a 99% reduction in cadmium (Cd) content and approximately 80% reduction in lead (Pb) content in both analyzed conditions. These values correspond to final concentrations of approximately 20 ppm of Cd and 1162 ppm of Pb. Therefore, from the perspective of current regulations, the obtained calcined product meets the necessary requirements for being directed to the agricultural market.

For future studies, tests will be conducted without the use of calcium chloride to minimize the potential for atmospheric emissions of chlorinated compounds. Atmospheric measurements are also planned to be conducted at the pilot rotary kiln chimney to monitor emissions of particulate matter, SOx, NOx, fluorides, dioxins, and furans. Finally, agronomic value tests will be carried out on agricultural crops over a period of 90 days to validate the potential use of the generated material as an effective fertilizer.

Professional summary:

- Isabela Correia Costa: Chemical Engineer with experience in sustainability and environmental management.

- Saulo Luiz Sales Parreiras de Rezende: Metallurgical Engineer with experience as an innovation project manager in the mining and metallurgical sector.

- Henrique Hipólito Costa: Chemical Engineer with experience in decarbonization projects.

References:

Brasil. Ministério da Agricultura, Pecuária e Abastecimento. “Instrução Normativa nº 27, de 5 de junho de 2006. Aprova os métodos analíticos oficiais para análise de corretivos de solo”. 2006. Anexo I.

Empresa Brasileira de Pesquisa Agropecuária (Embrapa). “Plano Diretor da Embrapa: 2024-2030”. 2023. https://www.embrapa.br/busca-de-publicacoes/-/publicacao/1163372/plano-diretor-da-embrapa-2024-2030.

Fundação Estadual do Meio Ambiente (Feam). “Inventário de resíduos sólidos da mineração: ano base 2017”. 2018. https://feam.br/w/inventario-de-residuos-solidos-minerarios.

Instituto Brasileiro de Mineração (IBRAM). “Panorama do Setor Mineral Brasileiro 2024”. 2024. https://panoramamineracao.com.br/pmb2024/.

Olszak-Humienik, M., Jablonski, M. Thermal behavior of natural dolomite. J Therm Anal Calorim 119, 2239–2248 (2015). https://doi.org/10.1007/s10973-014-4301-6.

VITERAGRO. “As 5 vantagens da aplicação da mistura de calcário e gesso”. 2022. https://viteragro.com.br/as-5-vantagens-da-aplicacao-da-mistura-de-calcario-e-gesso.