PERUMIN 37 Mining Convention

Arequipa, September 22 – 26, 2025

TECHNOLOGY, INNOVATION AND SUSTAINABILITY FORUM

CALL FOR TECHNICAL PAPERS

NATIONAL MINING AWARD

# Title: Enhancing Water Recovery in Mining Operation:  A Case Study from a Copper Mine Trial in Peru

Topic: Solid/Liquid Separation Operations

Category: Mineral Processing and Extractive Metallurgy.

Author: Ronny Guido García Mallqui, SNF Peru, Technical Advisor, Av. José pardo 434 Miraflores, rogarcia@snf.com, 970974091.

Co-authors: Trong Dang Vu, SNF, Mining R&D Manager, Canada, TDangVu@snf.com, +1(437) 9796869. Juan José Cahuana Cuba, Angloamerican Quellaveco, Process Manager, Peru, Juan.cahuana@angloamerican.com, 996328351.

Keywords: Water recovery improvement, rheology modifier, innovative flocculant, tailings management, mining efficiency enhancement.

# SUMMARY

# Water resource management and environmental risk mitigation are among the most critical challenges facing today’s mining industry. These issues are especially pressing in water-scarce region experiencing rapid mining expansion, such as Peru. Many mining companies are actively pursuing new technologies to enhance water recovery, particularly from tailings, and to recycle it back to the process. Improving water recovery not only conserves a vital resource but also reduces the volume of tailings discharged into the tailing’s storage facilities, thereby lowering the associated environmental risk.

# While mechanical technologies such as filter press and centrifuges are commonly explored, chemical approaches are also gaining increasing attention. This paper presents a case study of a chemical solution trialed at a full-scale copper mining operation in Peru between January 29th to February 08th, 2025. A newly developed water-soluble polymer flocculant, TFA, was tested against the incumbent flocculant in the tailing’s thickener.

# The trial results clearly demonstrated that the new TFA flocculant significantly improved the water recovery for the thickening circuit as compared to the conventional flocculant. At the same dosages of 11.5 g/t, the TFA flocculant increased water recovery by 8% as compared to conventional flocculant. The maximum solids content of the thickener underflow was 49% with the incumbent flocculant, compared to 52% for the TFA product. This increase in solids content enabled an additional 560 m3/h of water to be recovered. Continuous monitoring of key operating parameters revealed a notable increase in solids content of the underflow, enabling the recovery of greater volume of water. Moreover, the innovative chemistry of TFA allowed the thickener to operate at a higher solids content of the underflow without requiring modification to the underflow pumping system. The improvement not only enhanced the operation’s water sustainability but also opens the possibility of increasing ore processing in the future by securing a larger volume of recovered water. This study demonstrates the potential of chemical innovation such as TFA to significantly enhance water management practices in mining operations.