Optimización de tratamiento de minerales de cobres secundarios

Uno de los principales problemas en la unidad El Brocal, es el procesamiento de los minerales de cobre secundario, los cuales han incrementado a medida que se profundiza la extracción en la mina subterránea hacia la parte sur, esto ha impactado negativamente en la recuperación y calidad final del concentrado de cobre.

A raíz del problema mencionado, en coordinación con las áreas de Geología y Planeamiento se realizó una clasificación obteniendo 3 tipos de dominios para los minerales secundarios, en función al ratio Cu / As con valores de 4 para el domino 1, entre 4 y 8 para el dominio 2 y mayores a 8 para el dominio 3. En función a esto se realizaron pruebas metalúrgicas que indicaron que a medida que aumenta esta proporción de Cu/As para los minerales secundarios los resultados metalúrgicos varían negativamente.

Las investigaciones realizadas han permitido que se obtenga mejoras de los resultados modificando el pH de flotación, las dosis, puntos de adición de los reactivos e incluso modificando los colectores por unos más selectivos, los cuales mostraron una separación entre el Fe y el Cu según las pruebas de cinéticas de flotación.

Los análisis microscópicos y mineralógicos realizados indicaron una notoria variación de los minerales aportantes de cobre siendo para los minerales típicos una proporción de 90% de enargita y disminuyendo hasta valores de 9% en el dominio 3, y obteniendo a su vez proporciones mayores a 80% de cobres secundarios, preponderando la covelita y digenita .

La clasificación realizada se extendió a los diferentes tipos de minerales de cobre de la mina subterránea, obteniendo una clasificación de Cu/As que, validado por pruebas de flotación cíclicas de laboratorio, permitieron una mejor operación a nivel industrial. La separación de estos materiales por campañas e identificados desde mina, han mitigado el problema comercial con valores de concentrado menor a 12%, los cuales no eran comercialmente vendibles.

El conocimiento de los materiales que tienen un bajo rendimiento metalúrgico ha permitió que en las operaciones de mina, se realice una planificación más organizada sin dejar de obtener como meta el cumplimiento del Budget de finos metálicos ya establecidos para el presente año.

Optimization of secondary copper ore processing

One of the main problems at the El Brocal unit is the processing of secondary copper minerals, which has increased as extraction deepens in the underground mine toward the southern part. This has negatively impacted the recovery and final quality of the copper concentrate.

As a result of this problem, in coordination with the Geology and Planning departments, a classification was performed, resulting in three types of domains for the secondary minerals, based on the Cu/As ratio, with values ​​of 4 for domain 1, between 4 and 8 for domain 2, and greater than 8 for domain 3. Based on this, metallurgical tests were performed, which indicated that as the Cu/As ratio for secondary minerals increases, the metallurgical results vary negatively.

The research conducted has led to improved results by modifying the flotation pH, dosages, reagent addition points, and even by modifying the collectors to more selective ones, which showed a separation between Fe and Cu according to flotation kinetic tests.

The microscopic and mineralogical analyses performed indicated a notable variation in the copper-contributing minerals, with a 90% proportion of enargite for the typical minerals, decreasing to 9% in domain 3, and also obtaining proportions greater than 80% of secondary copper, with covellite and digenite predominating.

The classification was extended to the different types of copper minerals in the underground mine, obtaining a Cu/As classification that, validated by laboratory cyclic flotation tests, allowed for improved operations at the industrial level. The separation of these materials through campaigns and identification at the mine has mitigated the commercial problem with concentrate values ​​below 12%, which were not commercially saleable.

Knowledge of the materials with low metallurgical yield has allowed for more organized planning in mine operations while still achieving the target of meeting the fine metal budget already established for the current year.